SECTION 05600 – ALUMINUM COLUMN COVERS

Items noted (in parenthesis and italic text) are optional

or variable depending on individual job conditions.

PART 1 -GENERAL

1.01 SCOPE OF WORK

A.     Furnish all labor, materials and equipment to install column covers as shown on the contract drawings and as specified herein.

1.02 RELATED WORK

A.     Structural Metal Framing, Section 05 _______.

B.     Structural Framing Systems, Section 05 _______.

C.     Sealants, Section 07 _______.

D.     Exterior Finish System, Section 09 _______.

1.03 DESCRIPTION OF WORK

A.     Provide formed metal column covers and beam wraps in accordance with the contract drawings and details to insure a weathertight system. Metal column cover supplier shall be responsible for the design of all column cover systems including but not limited to the anchorage details, sealant recommendations, extrusions and flashings.  Contractor to coordinate requirements, quantities and sizes with structural drawings.

1.04 REFERENCE STANDARDS

A.     SMACNA

1. Architectural Sheet Metal Manual

B.     NAAMM

1. Metal Finishes Manual

1.05 SUBMITTALS

A.     Product Data: Submit manufacturer's specifications and installation instructions

for products, including finishes.

B.     Color Selection: Submit color chart showing full range available from

manufacturer's standard colors.

C.     Shop Drawings: Submit shop drawings for approval. Include all information

necessary for fabrication and installation of column covers. Indicated materials, sizes, thickness, fastenings, and profiles.

D.     Samples: Submit 2" X 3" metal samples of each required finish.

E.     Fabrication Qualifications: Furnish evidence that the proposed fabricator of this

work has a minimum of 5 years experience fabricating, finishing and installing similar 		work.

F.	Submit finish maintenance instructions.

1.06 DELIVERY, STORAGE AND PROTECTION

A.	Deliver, store and handle products to avoid any distortion or damage due to moisture, physical abuse or other cause. Column covers shall be free from nicks, scratches, and blemishes. Replace or repair defective or damaged materials as required.

1.07 QUALITY ASSURANCE

A.     Submit certification that system conforms to wind loading requirements of this specification.

B.	Submit mill certifications documenting that the physical properties of the metal used in the manufacturing of the column covers meets the specified requirements.

PART 2 PRODUCTS

2.01 COLUMN COVERS

A.     Provide AP-COL Aluminum column covers and Beam Wraps as manufactured

by Protean Construction Products, Inc. of Burnsville, MN. Phone: (952)895-4000,

Fax: (952)895-1691. www.protean.com

- Furnish and install where indicated or as specified on the drawings Protean

roll-formed aluminum column covers. Covers shall be .125" aluminum 5005 or 3003 alloy (16 ga stainless steel). Top and bottom rings shall be 1" .125" aluminum routed to inside radius of cover. Rings shall be attached by welded construction. Horizontal and vertical caulking reveals shall be a minimum of 1/2" wide. Fold back ends of metal to form a 2" wide attachment return leg on the concealed side. All exposed surfaces to be covered with PVC coating after paint finishing for protection from burnishes and scratches during ship and installation.

C.	Joint options:

1. AP-COL-100 minimum 1/2" joint with backer rod and sealant.

2. AP-COL-200 tight joint.

3. AP-COL-300 minimum 1/2" joint with formed metal joint closure.

2.02 MATERIALS

A.     Aluminum Sheet: ASTM B209 Alloy 5005 or 3003 with temper as required for

forming, or as otherwise recommended by metal producer to provide required finish.

(Stainless Steel Sheet: Type 304 or Type 316)

B.     Aluminum Extrusions: ASTM 8221, Alloy-6063-T5.

C.     Fasteners: Provide stainless steel screws and fasteners in 304 alloy unless otherwise indicated.

D.	Sealants: All sealants shall be in accordance with the latest ASTM standard

and shall comply with the sealant specifications of the contract documents. Apply

sealants in compliance with ASTM standards and sealant manufacturer’s

recommendations.

2.03 FABRICATION

A.     Size:

1.     Fabricated column covers to outside dimensions and radius indicated.

B.     Field Measurements:

1.	     Verify size; location and placement of column cover units prior to fabrication.

C.     Shop assembly:

1.     Each course to be fabricated in two or more sections with joints as

indicated on the drawings. Fold back end of metal to form a return leg and

attachment flange on the concealed side. Available joint options are sealed,

tight or open with formed metal closure to conceal attachment.

2.     Design and fabricate work to permit it’s Installation on fully concealed

mounting devices. Design and fabricate exterior items for thermal movement

caused by a surface temperature variation of 120 Degrees F without wrinkling,

buckling, leaking, causing undue stress on its fasteners, or other detrimental

effects. Fabricate the work to permit thermal movement within each individual

component without the need for separate expansion joints.

3.     Form bent, metal corners to the smallest radius possible without causing grain separation or otherwise damaging the work.

4.     Provide straps, plates and brackets as required for support and anchorage of fabricated items.

2.04 FINISHES

A.     Column covers shall be factory finished in an organic coating.

B.     Organic Coating: Clean and prime exposed aluminum surfaces and apply a

coating of Kynar 500/Hylar 5000 2-coat finish conforming to AAMA 605 in a standard

or custom color. Minimum dry film thickness shall be 1.2 mil or other finish as

selected by Architect (Anodized finish Class I Clear, Class I Bronze, or As Selected

by Architect) or (stainless steel #4 Brushed or #8 Polished), etc.

2.05 PROTECTION

A.     All exposed surfaces to be covered with PVC coating after finishing for protection from burnished and scratches during shipment and installation.

PART 3 EXECUTION

3.01 INSPECTION

A.	Examine structure and surfaces for defects that would prevent proper

installation and erection of column covers. Report any discrepancies to the Architect

and Contractor. Do not proceed until the situations have been corrected.

B.     Assure that leakproof connections can be made in surfaces as prepared by

other trades.

- All sizes to be field-verified by the Contractor prior to fabrication. Coordinate

changes in column cover locations and structural framing to allow for proper installation.

3.02 INSTALLATION

A.     Install in accordance with shop drawing submittals and manufacturer's written instructions.

3.03 CLEANING

A.     Touch-up damaged finishes.

B.     Cleaning and maintenance per manufacturer's maintenance instructions.

# Text boxes

Aluminum Column Covers AP-COL