| Prōtean | Extruded Aluminum Sunscreens SS – 310 |
| --- | --- |
| Construction Products, Inc. | Guide Specifications |

SECTION 10705 – EXTRUDED SUNSCREENS

PART 1 - GENERAL

1.1	SUMMARY

A. 	WORK INCLUDED: Provide materials, labor, equipment and services necessary to furnish, deliver and install all sun shades as shown on the drawings and as specified in this Section.

B.		RELATED DOCUMENTS: Drawings and general provisions of contract, including general and supplementary conditions and Division. l specification sections, apply to work of this section.

1.2.	PERFORMANCE REQUIREMENTS

A.		Provide exterior sun control assemblies capable of withstanding the effects of loads and stresses from dead loads, live loads, snow and wind loads and normal thermal movement without permanent deformation of assembly or components including blades, frames, and supports; noise or metal fatigue caused by blade rattle or flutter; or permanent damage to fasteners and anchors.

1.3		SUBMITTALS:

A.		Product Data: Submit manufacturer's specifications, technical data, and installation instructions for required products, including finishes.

B.	Shop Drawings: Submit shop drawings for fabrication and erection of screen units and accessories. Include plans, elevations, and details of sections and connections to adjoining work. Indicate materials, finishes, fasteners, joinery, and other information to determine compliance with specified requirements.

  - QUALITY ASSURANCE

- Engage an installer who has not less than 5 years experience in product installation.

- Assemblies should conform to all applicable code requirements.

  - DELIVERY, STORAGE, AND HANDLING

- Deliver materials to the project site ready for use and fabricated in as large sections and assemblies as practical, in unopened original factory packaging clearly labeled to identify manufacturer.

  - PROJECT CONDITIONS

A.	Field Measurements:  Verify actual supporting and adjoining construction by field measurements before fabrication; and indicate recorded measurements on final Shop Drawings.  Coordinate construction to ensure that sun control assemblies fit  properly to supporting and adjoining construction and coordinate schedule with construction progress to avoid delaying the work.

PART 2 - PRODUCTS:

2.1 	ACCEPTABLE MANUFACTURERS:

A.		Protean Construction Products, Inc, 11901 Riverwood Drive, Burnsville, MN 55337, phone (952)895-4000, fax (952) 895-1691.  www.protean.com

2.2 		MATERIALS:

A.	Aluminum extrusions: ASTM B 211, Alloy 6063-T5 or T-52.

B.	Clip Angles: Structural grade aluminum.

C.	Fastenings: Fasteners shall be aluminum or stainless steel. Provide types, gauges, and lengths to suit unit installation conditions.

D.	Anchors and Inserts: Use nonferrous metal or hot-dip galvanized anchors and inserts for installation and elsewhere as required for corrosion resistance. Use stainless steel or lead expansion bolt devices for drilled in place anchors. Furnish inserts, as required, to be set into concrete or masonry work.

2.3 FABRICATION, GENERAL:

- Provide custom designed, cantilevered sunshade and accessories of design, materials, sizes, depth, arrangement, and metal thickness as indicated or as required for optimum performance with respect to strength, durability, and uniform appearance.

- Include anchorages, and accessories required for complete assemble.

2.4 SCREEN CONSTRUCTION:

A.		Manufacturer’s:  Subject to compliance with requirements, manufacturers offering products that may be incorporated into the work include, but are not limited to the following:

1.	SS-310 as manufactured by PROTEAN CONSTRUCTION PRODUCTS, INC. and as shown on drawings.

2.  Pre-approved manufacturers.

B.	Extruded aluminum blades to be fabricated from on-piece 6063-T5 alloy extrusions, minimum 0.081 inch thick.  Outriggers to be fabricated from aluminum plate 6063-T5 alloy extrusions or aluminum plate materials.

2.5 ALUMINUM FINISH:

A.		General: Comply with NAAMM "Metal Finishes Manual" for finish designations and application recommendations, except as otherwise indicated. Apply finishes in factory after products are assembled. Protect finishes on exposed surfaces prior to shipment. Remove scratches and blemishes from exposed surfaces, which will be visible after completing finishing process.

B.		Provide Color as indicated or, if not otherwise indicated, as selected by architect from standard Kynar 500 colors.

C.		Fluorocarbon Coating: Inhibitive thereto-cured primer, 0.2 mil minimum dry film thickness, and thereto-cured fluorocarbon coating containing "Kynar 500" resin, 1.0 mil minimum dry film thickness.

D.		Furnish manufacturer's twenty (20) year guarantee of "Kynar 500" finish.

E.	        Finish shall be applied in the plant of the manufacturer

PART 3 - EXECUTION:

3.1			INSTALLATION:

A.	Locate and place screen units plumb, level, and in proper alignment with adjacent work.

B.	Use concealed anchorages wherever possible.

C.	Form tight joints with exposed connections accurately fitted together.

- Use isolation tape where aluminum comes in contact with steel or concrete.

  - CLEANING AND PROTECTION

- Periodically clean exposed surfaces of sun control devices that are not protected by temporary covering to remove finger prints and soil during installation period.

- Clean exposed surface with water and a mild soap not harmful to finishes.  Thoroughly rinse surfaces and dry.

- Protect sun control assemblies from damage during construction.  Use temporary protective coverings where needed and approved by the sun control manufacturer.  Remove protective covering upon completion of installation.

End of section.

| Prōtean |  |
| --- | --- |
| Construction Products, Inc. 11901 Riverwood Drive, Burnsville ,MN 55337 PHONE (952) 895-4000 FAX (952) 895-1691 | To the best of our knowledge, the information contained herein is accurate, however, Protean Construction Products, Inc. assumes no liability for the same and reserves the right to modify or Withdraw any information or products contained herein, without notice.. Printed in the U.S.A 3/8/00 |